## Slide 1: Semiconductor Heterostructures of monolayer transition metal dichalcogenides
Jacob Townson
Dr. Gutierrez’s
Condensed Matter Experimental Group

## Slide 2: Index
Definitions
Introduction
Synthesis of Materials
Data Analysis
Experience
References

## Slide 3: Definitions
Heterostructure- combination of multiple heterojunctions
Heterojunction- interface that occurs between 2 layers of dissimilar crystalline semiconductors
Band Gap- energy range in a solid where no electron state can exist, in between a valence band and conduction band
Notes: For chemistry people, on valence and conduction bands, think orbitals

## Slide 4: Definitions
Chalcogenide- chemical compound consisting of at least one chalcogen (Sulfur, Selenium, Tellurium) anion and at least one more electropositive element (ex. MoS2)
Substrate - the surface or material on which a material grows (what we make our films on)
TMD – Transition Metal Dichalcogenide

## Slide 5: Introduction - Materials
M= Transition Metal
X = Chalcogen
42
Mo
Molybdenum
74
W
Tungsten
8
O
Oxygen
16
S
Sulfur
34
Se
Selenium
52
Te
Tellurium

## Slide 6: Introduction – Band Gaps
Ref. 1 Extraordinary Room-Temperature Photoluminescence in Triangular WS2 Monolayers
-Humberto R. Gutiérrez et al., 2012
Electronic Band Structure of WS2
Note: Bottom is valence band, Top is conduction band
Notes: Material is direct if Direct Band Gap is smaller than Indirect, and the Indirect can’t actually be calculated experimentally. Indirect transition changes momentum, direct transition only changes energy. Phonon tranfers momentum to electron in Indirect transition.

## Slide 7: Introduction - Applications
Can be used for things such as solar cells
Optoelectric Devices
Other Low-Power Electronics
Solar Cell Layout:
Ref. 2 Extraordinary Sunlight Absorption and One Nanometer Thick Photovoltaics Using Two-Dimensional Monolayer Materials- Marco Bernardi et al, 2013

## Slide 8: Introduction – Structure
Hypothetical 2D Stacked Crystal Heterostructure
Ref. 3 Two-dimensional crystals-based heterostructures: materials with tailored properties- K. S. Novoselov and A .H. Castro Neto, 2012
Inplane Heterostructure layout

## Slide 9: SYNTHESIS
Experimental Techniques
  Substrate Cleaning
  Thermal Evaporation
  Atmospheric Chemical Vapor Deposition (CVD)
  Spin Coating
  KOH Assisted Film Transfer

## Slide 10: Synthesis – Substrate Cleaning
Our films are deposited on
Before any depositing or growth, we clean substrates through a sonic bath with acetone then putting it in Piranha solution.
Si Substrate
Notes: Should I call this Piranha?

## Slide 11: Synthesis – Thermal Evaporation
MoO3 or WO3
over Si
The material in the boat goes through sublimation. Using this method, we deposit a single layer of the Transition Metal’s Oxide to the substrate.
Boat heated up to high temperatures

## Slide 12: Synthesis - CVD
Chemical Vapor Deposition
MoO3 or WO3
Chalcogen
N2 or Ar+H
Three separate temperature controlled zones
Using the CVD, we deposited the chalcogen atoms to the substrate with the tranistion metal, making a TMD.

## Slide 13: Synthesis – Different Processes
Series A (substrates-SiO2/Si, Si <111>, Sapphire)
  Thermal evaporation of 1 to 4 layer amorphous MoO3 (at 10-5 Torr) with 7.5 x 7.5 μm or 19 x 19 μm mesh TEM grids.
  Thermal evaporation of 1 to 4 layer amorphous WO3 (at 10-5 Torr) without grids.
  Sulfurization, Selenization, or Tellurization in three zone quartz tube furnace
Series B (substrates-SiO2/Si, Si <111>, Sapphire)
  Thermal evaporation of 1 to 4 layer amorphous MoO3 (at 10-5 Torr) with 7.5 x 7.5 μm or 19 x 19 μm mesh TEM grids.
  Sulfurization, Selenization, or Tellurization in three zone quartz tube furnace
  Thermal evaporation of 1 to 4 layer amorphous WO3 (at 10-5 Torr) without grids.
  Sulfurization, Selenization, or Tellurization in three zone quartz tube furnace

## Slide 14: Synthesis – Different Processes
(1) MoO3 Thermal Evaporation
(2) Mask removal
(2B) Chalcogenization
(3) WO3 Thermal Evaporation
(4) Chalcogenization
Heterostructure
Series A
Series A
Series B
MoX2
WX2
WX2
WX2
WX2
WX2
WyMo1-yX2
WyMo1-yX2
Heterostructure
Series B
X = S, Se or Te
Notes: Series A and B are stacked and in plane, series A with a lot of alloying, series B with little to no alloying

## Slide 15: Synthesis – Spin Coating
Using the Spin Coater, we would spread a layer of PMMA over the substrate with the film on top. By doing this, we could then do a film transfer (next slide) to put our film on a different substrate such as glass for Optical Absorption Testing

## Slide 16: Synthesis - KOH Assisted Film Transfer
(a)
(b)
TMD film
transferred to
a glass substrate
Using KOH, we could remove the film with little to no damage to a different substrate.

## Slide 17: Synthesis – Different Processes
Series C (substrates-SiO2/Si, Si <111>, Sapphire)
  Thermal evaporation of 1 to 4 layer amorphous MoO3 (at 10-5 Torr) onto substrate.
  Thermal evaporation of 1 to 4 layer amorphous WO3 (at 10-5 Torr) onto another substrate.
  Sulfurization, Selenization, or Tellurization in three zone quartz tube furnace of each sample
  Transfer one film and place that sample on top of the other sample

## Slide 18: Synthesis – Different Processes
(1) TMD1, after thermal evaporation and Chalcogenization
Series C
TMD2
TMD1
(1) TMD2, after thermal evaporation and Chalcogenization
(2) Coat TMD1 with PMMA
(3) Detach PMMA/TMD1 from substrate using KOH
(4) Retrieve PMMA/TMD1 with TMD2
(5) Remove PMMA with Acetone
Heterostructure
Series C
Notes: Series C are purely stacked heterostructures with no alloying

## Slide 19: Data Analysis
Raman Spectroscopy
Optical Absorption
Not included:
  TEM (Transmission Electron Microscopy)
  AFM (Atomic Force Microscopy)

## Slide 20: Analysis – Optical Microscope
  7.5 x 7.5 μm grids. 50x magnification.
Series A WS2/MoS2
Here we can clearly see the squares from the TEM grids used for series A and B
Notes: Move up next to series A and B

## Slide 21: Analysis – Raman
Raman Spectroscopy is a technique used to observe low-frequency modes in a system
It is the inelastic scattering of photons after interacting with the molecular vibrations or phonons in our system
E = 0
Intermediate State
Excited Vibrational States
hνi
hνf
Vibrational
Ground State
hνi
hνf
Excited Vibrational States

## Slide 22: Analysis - Raman
Raman Active modes for transition metal dichalcogenides
1 layer
We only use the and modes. The rules as to why are obtained from group theory in the back scattering of the photons.
Ref. 8 Photoluminescence emission and Raman response of monolayer MoS2, MoSe2, and WSe2- Philipp Tonndorf et al., 2013
Ref. 9 Raman and resonance Raman investigation of MoS2 nanoparticles- Gitti L. Frey et al., 1999
Ref. 10 Anomalous Lattice Vibrations of Single and Few-Layer MoS2- Changgu Lee et al., 2010
It is important to note that the modes could shift in frequency depending on how many layers of a substance are on a film.
Notes: Give example of mode shift from Mo multiple layer problems

## Slide 23: Analysis - Raman
What can Raman show us?
  What materials we have in our film
  The number layers of a certain substance
  The effect of possible alloying in our films

## Slide 24: Analysis – Raman (Example)
WSe2-MoSe2
MoSe2
WSe2
Series A
Series B
WS2-MoS2
MoS2
WS2
Series A
Series B
(a)
(b)
1
2
1
2
1
1
2
1
1
2
Notes: Note, in this example, Mo is in bulk (not single layer), but this is used to clearly show effects of alloying

## Slide 25: Analysis - Raman
WS2/MoS2 Series C Bilayer
MoS2 monolayer used in
Series C
WS2 monolayer used in
Series C
WS2/MoS2 Series A
WS2/MoS2 Series B
WS2/MoS2 Series C
E12g
WS2
E12g
MoS2
A1g
MoS2
A1g
WS2
Series C
Notes: We can see properties of alloying in Series A, a little bit in Series B, and none in Series C

## Slide 26: Analysis – Optical Absorption
Optical Absorption is a technique used to measure either the absorbance or percent transmission of a material.
Because our films are transparent, this is used as a method for determining the band gap.
In order to use this method, we had to put our films on glass (a transparent substrate), then account for the glass in our final calculations.

## Slide 27: Analysis – Optical Absorption
Absorption/Transmission
I0
Isub
Substrate
I0
Isub
Sample
Isub_sam
Define Terms
I0= initial intensity
Isub= intensity after transmitting
through substrate
Isub_sam=intensity after transmitting
through substrate and sample

## Slide 28: Analysis – Optical Absorption
According to the software we used to measure absorbance and transmission, these are the equations for each:
Absorbance
  ABS=2-log10(%T)
Transmission
  T = Iexit/Iinitial
  %T=(Iexit/Iinitial)*100
  Iexit = measured exit intensity
  Iinitial = measured reference intensity
By combining these equations, we found that to account for the glass substrate we had to divide the Transmission through the sample on the glass by the Transmission through the glass by itself
Notes: Lambda 950 UV/Vis Spectrometer, PerkinElmer UV Winlab software

## Slide 29: Analysis – Optical Absorption
  ref.6
  α= absorption coefficient of material
  I= Intensity of light beam
  = incident photon energy
  x= propagation path
  Beer-Lambert Law
We get the Beer-Lambert Law from the absorption coefficient equation through DE. This gives us the relationship between intensity, absorption coefficient, and film thickness.
Notes: Alpha- relative decrease of the photon energy along the propagation path

## Slide 30: Analysis – Optical Absorption
=
By using the Beer-Lambert Law with the equations given to us from the software, we were able to find the equation for absorption coefficient that relates it to absorbance and transmission.

## Slide 31: Analysis – Optical Absorption
Film thickness is still needed to calculate absorption coefficient.
  Film thickness was estimated by using theoretical values of distance from midpoint of a chalcogen atom to midpoint of another chalcogen atom directly below it on the c-axis. The excluded pieces of the chalcogen atoms are then added on to the thickness.
Ref 19. First principles study of structural, vibrational and electronic properties of graphene-like MX2 (M=Mo, Nb, W Ta; X= S, Se, Te) monolayers- Yi Ding et al., 2011
Ref 20. Electronegativity and Bond Energy - R. T Sanderson et al., 1983
h
rc
rc
chalcogen
transition metal
h = distance from midpoints of two chalcogen atoms
along vertical axis
rc = covalent radius of chalcogen atom

## Slide 32: Analysis – Optical Absorption
Table 2:
Values used for film thickness d
 | h (angstrom) Ref. 19 | rc (angstrom) Ref. 20 | d (angstrom)
WS2 | 3.14 A | 1.05 A | 5.24 A
MoS2 | 3.13 A | 1.05 A | 5.23 A
WSe2 | 3.36 A | 1.20 A | 5.76 A
MoSe2 | 3.35 A | 1.20 A | 5.75 A
=
  These d values relate back to absorption coefficient, thus giving us all we need to find it

## Slide 33: Analysis – Optical Absorption
=
  Ref.13-18
  α = absorption coefficient
  hν = incident photon energy
  A= constant
  Eg= energy gap of semiconductor
Ref 13. Band gap determination using absorption spectrum fitting procedure- Nader Ghobadi, 2013
Ref 14. Optical Band Gap Studies of Tungsten Sulphoselenide Single Crystals Grown by a DVT Technique- D.A. Dholakia et al., 2003
Ref 15. Optical Properties of Thin Semiconductor Films- Grolik Benno, Kopp Joachim, 2003
Ref 16.CdTiO3 thin films from an octa-nuclear bimetallic single source precursor by aerosol assisted chemical vapor deposition- Shahzad Abu Bakar et al., 2012
Ref 17. Optoelectronics, by E. Rosencher, 2002, equation (7.25)
Ref 18.Optical Processes in Semiconductors- Jacques I. Pankove, 1971
Given this equation, we can now relate all of our information to the direct band gap.
Note: hv can be obtained by it’s relation to wavelength

## Slide 34: Analysis – Optical Absorption
In this reference, it can be seen how to calculate the band gap: by extrapolating the linear portion of the graph. The x-intercept of the linear portion is the value of the direct band gap. The x intercept of the tail of the graph is the indirect band gap.
Ref 14. Optical Band Gap Studies of Tungsten Sulphoselenide Single Crystals Grown by a DVT Technique- D.A. Dholakia et al., 2003
Notes: We plot (alpha*hv)^(1/r) where in our case r = ½ vs. eV (photon energy)

## Slide 35: Analysis – Optical Absorption
This is the Absorbance scan done of glass by itself. Around 1.5 there is a change made in the spectrometer that can’t be avoided (under further investigation). Because of this, that area with scattered data will be in all samples.

## Slide 36: Lambda 950 schematics

## Slide 37: Analysis – Optical Absorption
WS2 Monolayer
Eg= 2.199eV
Direct Transition
Notes: Material is direct if Direct Band Gap is smaller than Indirect, and the Indirect can’t actually be calculated experimentally. We know monolayers to only be direct. Can see exiton because we have a single layer film, if it were bulk, we would not be able to see this.

## Slide 38: Analysis – Optical Absorption
WSe2/MoSe2 Bilayer Heterostructure Series A
Eg = 1.806 eV
Direct
Eg= 1.124 eV
Indirect

## Slide 39: Analysis – Optical Absorption
Sample | Direct Eg Experiment | Indirect Eg Experiment | Eg Ref. 8 | Eg. Ref. 8 A Stacking | Eg. Ref. 8 B Stacking
WS2 monolayer | 2.199 eV |  | 1.940 eV |  | 
MoS2 monolayer | 1.829 eV |  | 1.823 eV |  | 
WSe2 monolayer | 1.722 eV |  | 1.676 eV |  | 
MoSe2 monolayer | 1.655 eV |  | 1.606 eV |  | 
WS2/MoS2 Series A | 1.990 eV | 1.573 eV |  | 1.695 eV | 1.708 eV
WS2/MoS2 Series B | 2.144 eV | 1.672 eV |  | 1.695 eV | 1.708 eV
WS2/MoS2 Series C | 1.489 eV | .795 eV |  |  | 
WSe2/MoSe2 SeriesA | 1.806eV | 1.124 eV |  | 1.443 eV | 1.471 eV
WSe2/MoSe2 Series B | Ongoing | Ongoing |  | 1.443 eV | 1.471 eV
WSe2/MoSe2 SeriesC | 1.86 eV | .759 eV |  |  | 
Ref 8. Novel hetero-layered materials with tunable direct band gaps by sandwiching different metal disulfides and diselenides

## Slide 40: Experience
Trained on CVD multiple zone furnaces
Trained on thermal evaporators
Trained in Raman spectroscopy
Trained in UV visible optical spectroscopy
Trained in vacuum systems
  Connection & gas lines, vacuum pumps (both mechanical & diffusion)
Trained in spin coating
Trained in semiconductor film transfer
Trained in substrate cleaning techniques
Exposure to both TEM and AFM

## Slide 41: REFERENCES
1.) Band gap determination using absorption spectrum fitting procedure
  Author: Nader Ghobadi
2.) Optical Band Gap Studies of Tungsten Sulphoselenide Single Crystals Grown by a DVT Technique
  Author: D.A. Dholakia, G.K. Solanki, S.G. Patel, and M.K. Agarwal
3.) Optical Properties of Thin Semiconductor Films
  Author: Grolik Benno, Kopp Joachim
4.)CdTiO3 thin films from an octa-nuclear bimetallic single source precursor by aerosol assisted chemical vapo deposition
  Author: Shahzad Abu Bakar, Syed Tajammul Hussain and Muhammad Mazhar
5.) Optoelectronics, by E. Rosencher, 2002, equation (7.25)-Wikipedia
6.)Optical Processes in Semiconductors, by Jacques I. Pankove, 1971
7.) Band offsets and heterostructures of two-dimenstional semiconductors
  Author: Jun Kang, Sefaattin Tongay, Jian Zhou, Jingbo Li, and Junqiao Wu
8.) Novel hetero-layered materials with tunable direct band gaps by sandwiching different metal disulfides and diselenides
  Author: Humberto Terrones, Florentino Lopez-Urias, and Mauricio Terrones

## Slide 42: REFERENCES
9.) First principles study of structural vibrational and electronic properties of graphene-like MX2 (M= Mo, Nb, W, Ta; X= S, Se, Te) monolayers
  Author: Yi Ding, Yanli Wang, Jun Ni, Lin Shi, Siqi Shi, Weihua Tang
10.) Electronegativity and Bond Energy
  Author: R. T. Sanderson

## Slide 43: Thank You